BAYDEE – TECHNICAL SPECIFICATIONS

Engineered UPVC Profiles • Profile Systems • Tested Performance

01 — Profile Series

Casement Series (link to casement series images)

50 mm — Profile thickness: 2.0 mm

60 mm — Profile thickness: 2.2 mm

Sliding Series (link to Sliding series images)

55 mm — Profile thickness: 2.2 mm

60 mm — Profile thickness: 2.2 mm

80 mm — Profile thickness: 2.2 mm

90 mm — Profile thickness: 2.2 mm

112 mm — Profile thickness: 2.2 mm

02 — Profile Construction

Multi-chamber design profiles

Precision profile geometry for window and door fabrication

Smooth and uniform visible surfaces

03 — Glazing

Single glazing

Double glazing

Glazing configurations to be selected according to the applicable profile system

04 — Sealing System

Compatible with weather-sealing gaskets

Improved air and water sealing

05 — Profile Dimensions & Quality

Tested profile depth: 60.0 mm

Tested profile width: 57.30 mm

Sight visible surface wall thickness: 2.40 mm

Non-sight visible surface wall thickness: 1.65 mm

Sight visible surface flatness: 0.25 mm

Parallelism: 0.4 mm

Straightness: 0.09 mm

Mass of profile: 1046 g/m

06 — Material & Surface Quality

Appearance: Complies

Colour: Same and uniform on all visible surfaces

Surface: Smooth and free from pitting, impurities, cavities and other surface defects

Edges: Clean and burr-free

Colour measurement: L = 93.89, a = -2.10, b = 1.32

07 — Mechanical Performance

Flexural Modulus of Elasticity: 2894 N/mm²

Tensile Bending Test (L-corner): 630 N

Compression Bending Test (L-corner): 1677 N

Resistance to Impact by Falling Mass: No deformation and no failure observed visually

08 — Thermal Performance

Vicat Softening Temperature at 5 kg load: 81.2 °C

Heat Reversion: 1.87%

Visual examination after heat ageing at 150 °C for 30 min: Complies

09 — Physical Properties

Mass of Profile: 1046 g/m

10 — Standards & Test Results

IS 17953: Profile performance, dimensions, wall thickness, surface quality, mechanical and thermal tests

ASTM D 2244: Colour Measurement

| Test | Standard | Result |
| --- | --- | --- |
| Vicat Softening Temperature at 5 kg Load | IS 17953 | 81.2 °C |
| Flexural Modulus of Elasticity | IS 17953 | 2894 N/mm² |
| Appearance | IS 17953 | Complies |
| Colour Measurement | ASTM D 2244 | L 93.89 / a -2.10 / b 1.32 |
| Heat Reversion | IS 17953 | 1.87% |
| Falling Mass Impact | IS 17953 | No deformation / No failure observed visually |
| Heat Ageing | IS 17953 | Complies |
| Tensile Bending – L-corner | IS 17953 | 630 N |
| Compression Bending – L-corner | IS 17953 | 1677 N |